ECE 162B – Homework #5		HALL EFFECT  P-N JUNCTON SEMICONDUCTORS

Due March 2,  2011 in class

____________________________________________________________________________________

Read Chapter 8 and start Chapter 9 in Solymar and Walsh

- Do Problem 8.9 in Solymar and Walsh

2.	Consider a Hall Sample of Silicon of Length L=0.1cm and Width W=0.01cm, and thickness of 0.001cm.  Assume also that x=1.0mA, Vx =12.5volts and Bz=500gauss=0.05Tesla.

The sample is doped with 1E16cm-3 acceptors and 3E+15cm-3 donors.

Calculate the Hall Voltage (Magnitude and sign) and the mobility of the carriers in the samples at 300K.

- Consider an n+-p diode fabricated from GaAs shown below, and given ni=2E+6cm-3 at 300K, and Eg=1.4eV.

Given that the Donor density is 1E+17cm-3 and acceptor density is 1E+16cm-3 in the n+ and p-material, respectively.

- Calculate the built-in voltage and depletion width of the junction given that the permittivity of GaAs is 13.1.

- Sketch the band diagram, charge density distribution, and electric field including approximate depletion widths.

Nd= 1E+17cm-3        Na=1E+16cm-3